Laboratory of Kinetic Phenomena in Solids at Low Temperatures 
Physics of tellurium 

Leading by
	


Iosif Farbshtein, Principal Researcher 


	


Vyaecheslav Berezovets, Senior Researcher
	


Robert Parfen'ev, Professor
	[image: image4.jpg]




 

 HYPERLINK "mailto:sergei.v.yakimov@mail.ioffe.ru" Sergey Yakimov, Junior Researcher


  

Goal: the study of the elementary semiconductor with a unique anisotropic structure. 
Objects: high quality single crystal Te and low-dimensional tellurium – based structures 
Methods: dc electric measurements of classical and quantum effects, measurements of optical activity, high pressure studies at 0.4 K< T
• High quality Te single crystals (extremely pure and doped by Sb) have been obtained by Czohralsky method. The peculiarities of crystal growth at different gravity levels have been determined.
 • Galvanomagnetic properties in low magnetic field and their dependence on the amount of structural defects have been investigated. 
• The shape of the hole Fermi surface in Tellurium and its evolution with concentration of careers have been determined. The dispersion law of the Te valence band have been calculated.
• The transformation of Te valence band by hydrostatic pressure have been measured. 
• The optical activity of tellurium near the band edge and optical translucence have been measured and compared with the developed theory. 
• The 2D layer on the different Te crystal surfaces have been created and the electronic spectrum of 2D holes have been determined by SdH effect. 
• The anomalous positive magnetoresistivity of 2D holes on different Te surfaces have been discovered and explained by the theory of weak localization of careers with pronounced anisotropy and without spin degeneracy as a result of high spin-orbital interaction. 
• Te nanocluster system in the voids of opal structure have been obtained and its galvanomagnetic properties have been investigated.
 
Crystal structure of tellurium

 [image: image5.jpg]




Parameters of tellurium crystal structure
[image: image6.png]a i ¢ i interatomic distances
in a chain between chains
445 591 2,86 3,74




[image: image7.emf]0 10 20 30 40

1

10

p, 10

14

cm

-3

q, mm

10

100

R



, 10

3

 cm

2

/V s

[image: image8.emf]0 10 20 30 40 50

10

100

p, 10

14

 cm

-3

q, mm

 W-mg

 W-1g

0

0,1

1

R

s

, 10

3

 cm

2

 V

-1

 s

-1

[image: image9.emf]

[image: image10.emf]0,01 0,1 1 10

1

10

1*

2

 

 

T, K

300   100             10                1                0.1

3*

3

2*

1

r

, 

W

 cm

1/T, K

-1

[image: image11.emf]D


i


D


i


L


p


CN


T


BN


AT


u


u


u


u


+


+


=


+


+


=


-


2


3


2


3


1


1


1


1




D i

D i L p

CN T BN AT

u u u u

     



2

3

2

3

1 1 1 1

[image: image12.emf]A


B


N


i


=p


D


D


e


*


m


u


1


t


=


N


D


Sample


V


s


cm


K


×


×


2


3


2


2


3


K


cm


s


V


×


×


×


cm


-3


cm


V


s


2


1


×


æ


è


ç


ö


ø


÷


-


cm


-3


SC-


m


g


3


×


10


-7


4.9


×


10


-19


4.1


×


10


14


9.3


×


10


-6


7.7


×


10


15


W-


m


g


3


×


10


-7


4.9


×


10


-19


1.2


×


10


15


1.0


×


10


-3


8.3


×


10


17


W-1g


0


3


×


10


-7


4.9


×


10


-19


1.1


×


10


15


6.0


×


10


-4


5.0


×


10


17


Opal<Te>


3


×


10


-7


4.9


×


10


-19


1.8


×


10


14**


1.5


×


10


-1


1.2


×


10


20




A B N i =p

D D

e

* m

u

1





N D Sample

Vs

cm K





2 32

2 3

K cm s V

  

cm -3

cm

Vs

2

1

















cm -3 SC-  g 3  10 -7 4.9  10 -19 4.1  10 14 9.3  10 -6 7.7  10 15 W-  g 3  10 -7 4.9  10 -19 1.2  10 15 1.0  10 -3 8.3  10 17 W-1g 0 3  10 -7 4.9  10 -19 1.1  10 15 6.0  10 -4 5.0  10 17 Opal<Te> 3  10 -7 4.9  10 -19 1.8  10 14** 1.5  10 -1 1.2  10 20

[image: image13.emf]1 10 100

0,01

0,1

1

10

opal <Te>

W-1g

0

SC-



g

W-



g

R

H

, 10

3

 cm

3

/ C

T, K

[image: image14.emf]1 10 100

0,01

0,1

1

10

100

1000

CN

D

CN

D

(W-1g

0

)

CN

D

(W-g)

A T

3/2

CN

D

(SC-g)

B N

i

 T

-3/2

W-1g

0

W-g

SC-g

opal <Te>

1/u, 10

-4

 cm

-2

/ V 

-1

 s

-1

T, K

[image: image15.emf]D


2


2


*


3


0


D


N


e


m


20


1


×


×


×


e


×


=


t


h




D

2 2*

3

0

D

N

e m

20 1





  







[image: image16.emf]D


D


e


*


m


u


1


t


×


=




D D

e

* m

u

1

 



[image: image17.emf]For 


Te:


e


0


 


 = 


e


e


11


2


33


3


0


(


)


= 33.82


m*/m


0


=


m


m


^


×


2


3


|


|


 = 0.156.




For  Te:  0    = 

 

11

2

33

3

0 ( )

= 33.82 m*/m 0 =

m m





2

3

||

 = 0.156.



[image: image18.emf]0 10 20 30 40

10

100

 W-



g  sample

 W-1g sample 

N

D

 , 10

16

 cm

-3

q, mm

1

10



300 K 

, Ohm cm 

100

1000

 

 

 

u=R



, cm

2

/ V s

[image: image19.emf]0 2 4 6 8

-6

-4

-2

0

2

4

6

8

10

12

14

16



0

, %

H, kOe

 W-1g

0

  (0.4 K)

 W-



g   (0.4 K)

 SC-1g

0

 (0.4 K)

 Opal<Te>   (1.5 K)

[image: image20.emf]4,0

4,1

Opal<Te>



, Ohm cm

H, kOe

5,2

5,3

W-1g

0

 

 

24,5

 

W-



g

 

0 1

0,15

0,16

0,17

SC-1g

0

 

 

[image: image21.emf]Conclusion


For the first time we have studied the temperature and magnetic field behavior of the electrical 


resistivity


and MR for two kinds of a block structure of 


Te: the 


microcrystalline structure in ingots grown during


rapid spontaneous solidification under 


microgravity conditions and the 


nanocluster Opal<Te> structure


formed after filling of the opal voids by melted 


Te.


-    In the case of complete melting and re-solidification of 


Te in 


m


g without a seed, the initial


undercooling of the melt followed by spontaneous nucleation and solidification resulted in a


microcrystalline structure with oscillating the neutral-defect concentration and crystalline orientation


along the ingot. The 


maxima of the 


resistivity 


r


300K


, as well as N


D


 profile correspond to the region of ingot


surface contacts with the walls ordinary appeared under 


m


g conditions.


-    The sensitivity of the electrical properties of 


Te at low temperatures to the distribution of both neutral


and electrically active defects allowed to determine the impurity and defect profiles along the ingot length


at the level of 10


-5


%, which could not be achieved by other methods.


-    The rough decrease of the hole mobility (in one order) and the positive AMR in low magnetic fields


for the W-


m


g ingot indicate the predominant hole scattering on neutral defects and boundaries (N


D


~10


18


cm


-3


).


-    In the opal<Te> samples we have got the regular structure of contiguous clusters of 


Те with 2D


conducting faces. The physical properties of such 2D conducting ordered system (low mobility, weak


localization effect, anisotropy) are determined by both the interface effects between the 


Те 


nano clusters


and the SiO


2


 amorphous spheres and the symmetry of the Te 


sublattice. The positive AMR of this


conducting system at low temperatures is a result of the interface scattering of 2D-holes in contrast to a


bulk 


Te crystal where AMR is always negative.




Conclusion For the first time we have studied the temperature and magnetic field behavior of the electrical  resistivity and MR for two kinds of a block structure of  Te: the  microcrystalline structure in ingots grown during rapid spontaneous solidification under  microgravity conditions and the  nanocluster Opal<Te> structure formed after filling of the opal voids by melted  Te. -    In the case of complete melting and re-solidification of  Te in   g without a seed, the initial undercooling of the melt followed by spontaneous nucleation and solidification resulted in a microcrystalline structure with oscillating the neutral-defect concentration and crystalline orientation along the ingot. The  maxima of the  resistivity   300K , as well as N D  profile correspond to the region of ingot surface contacts with the walls ordinary appeared under   g conditions. -    The sensitivity of the electrical properties of  Te at low temperatures to the distribution of both neutral and electrically active defects allowed to determine the impurity and defect profiles along the ingot length at the level of 10 -5 %, which could not be achieved by other methods. -    The rough decrease of the hole mobility (in one order) and the positive AMR in low magnetic fields for the W-  g ingot indicate the predominant hole scattering on neutral defects and boundaries (N D ~10 18 cm -3 ). -    In the opal<Te> samples we have got the regular structure of contiguous clusters of  Те with 2D conducting faces. The physical properties of such 2D conducting ordered system (low mobility, weak localization effect, anisotropy) are determined by both the interface effects between the  Те  nano clusters and the SiO 2  amorphous spheres and the symmetry of the Te  sublattice. The positive AMR of this conducting system at low temperatures is a result of the interface scattering of 2D-holes in contrast to a bulk  Te crystal where AMR is always negative.

[image: image22.jpg]


[image: image23.png]


[image: image24.png]


[image: image25.png]


[image: image26.wmf]0

10

20

30

40

1

10

p, 10

14

cm

-3

q, mm

10

100

R

s

, 10

3

 cm

2

/V s

[image: image27.wmf]0

10

20

30

40

50

10

100

p, 10

14

 cm

-3

q, mm

 W-

m

g

 W-1g

0

0,1

1

R

s

, 10

3

 cm

2

 V

-1

 s

-1


[image: image28.png]




[image: image29.jpg]


[image: image30.jpg]


[image: image31.jpg]


[image: image32.jpg]


[image: image33.jpg]



[image: image34.jpg]a8

r L - %‘
] L
.n’m‘ \ ¥




[image: image35.wmf][image: image36.jpg]'] 4 F 4

) :v:ww\uvu At 7.0
7l LU ea ey, {
7 Y10 s\\-.wt..\
e .\~:“\“f._>
V3 134 Fis i it EAe G

-
1
1

!

\
1\

-

-~
-
—

-

-~
-

T

-

-
e iy S

e





[image: image37.wmf]0,01

0,1

1

10

1

10

1*

2

 

 

T, K

300   100             10                1                0.1

3*

3

2*

1

r

, 

W

 cm

1/T, K

-1

[image: image38.wmf]D

i

D

i

L

p

CN

T

BN

AT

u

u

u

u

+

+

=

+

+

=

-

2

3

2

3

1

1

1

1

[image: image39.wmf]A

B

N

i

=p

D

D

e

*

m

u

1

t

=

N

D

Sample

V

s

cm

K

×

×

2

3

2

2

3

K

cm

s

V

×

×

×

cm

-3

cm

V

s

2

1

×

æ

è

ç

ö

ø

÷

-

cm

-3

SC-

m

g

3

×

10

-7

4.9

×

10

-19

4.1

×

10

14

9.3

×

10

-6

7.7

×

10

15

W-

m

g

3

×

10

-7

4.9

×

10

-19

1.2

×

10

15

1.0

×

10

-3

8.3

×

10

17

W-1g

0

3

×

10

-7

4.9

×

10

-19

1.1

×

10

15

6.0

×

10

-4

5.0

×

10

17

Opal<Te>

3

×

10

-7

4.9

×

10

-19

1.8

×

10

14**

1.5

×

10

-1

1.2

×

10

20

[image: image40.wmf]1

10

100

0,01

0,1

1

10

opal <Te>

W-1g

0

SC-

m

g

W-

m

g

R

H

, 10

3

 cm

3

/ C

T, K

[image: image41.wmf]1

10

100

0,01

0,1

1

10

100

1000

CN

D

CN

D

(W-1g

0

)

CN

D

(W-

m

g)

A T

3/2

CN

D

(SC-

m

g)

B N

i

 T

-3/2

W-

1g

0

W-

m

g

SC-

m

g

opal <Te>

1/u, 10

-4

 cm

-2

/ V 

-1

 s

-1

T, K

[image: image42.wmf]D

2

2

*

3

0

D

N

e

m

20

1

×

×

×

e

×

=

t

h

[image: image43.wmf]D

D

e

*

m

u

1

t

×

=

[image: image44.wmf]For 

Te:

e

0

 

 = 

e

e

11

2

33

3

0

(

)

= 33.82

m*/m

0

=

m

m

^

×

2

3

|

|

 = 0.156.

[image: image45.wmf]0

10

20

30

40

10

100

 W-

m

g  sample

 W-1g sample 

N

D

 , 10

16

 cm

-3

q, mm

1

10

r

300 K

r

, Ohm cm 

100

1000

 

 

 

u=R

s

, cm

2

/ V s

[image: image46.wmf]0

2

4

6

8

-6

-4

-2

0

2

4

6

8

10

12

14

16

Dr/r

0

, %

H, kOe

 W-1g

0

  (0.4 K)

 W-

m

g   (0.4 K)

 SC-1g

0

 (0.4 K)

 Opal<Te>   (1.5 K)

[image: image47.wmf]4,0

4,1

Opal<Te>

r

, Ohm cm

H, kOe

5,2

5,3

W-1g

0

 

 

24,5

 

W-

m

g

 

0

1

0,15

0,16

0,17

SC-1g

0

 

 

[image: image48.wmf]Conclusion

For the first time we have studied the temperature and magnetic field behavior of the electrical 

resistivity

and MR for two kinds of a block structure of 

Te: the 

microcrystalline structure in ingots grown during

rapid spontaneous solidification under 

microgravity conditions and the 

nanocluster Opal<Te> structure

formed after filling of the opal voids by melted 

Te.

-    In the case of complete melting and re-solidification of 

Te in 

m

g without a seed, the initial

undercooling of the melt followed by spontaneous nucleation and solidification resulted in a

microcrystalline structure with oscillating the neutral-defect concentration and crystalline orientation

along the ingot. The 

maxima of the 

resistivity 

r

300K

, as well as N

D

 profile correspond to the region of ingot

surface contacts with the walls ordinary appeared under 

m

g conditions.

-    The sensitivity of the electrical properties of 

Te at low temperatures to the distribution of both neutral

and electrically active defects allowed to determine the impurity and defect profiles along the ingot length

at the level of 10

-5

%, which could not be achieved by other methods.

-    The rough decrease of the hole mobility (in one order) and the positive AMR in low magnetic fields

for the W-

m

g ingot indicate the predominant hole scattering on neutral defects and boundaries (N

D

~10

18

cm

-3

).

-    In the opal<Te> samples we have got the regular structure of contiguous clusters of 

Те with 2D

conducting faces. The physical properties of such 2D conducting ordered system (low mobility, weak

localization effect, anisotropy) are determined by both the interface effects between the 

Те 

nano clusters

and the SiO

2

 amorphous spheres and the symmetry of the Te 

sublattice. The positive AMR of this

conducting system at low temperatures is a result of the interface scattering of 2D-holes in contrast to a

bulk 

Te crystal where AMR is always negative.














































Eg=0.33 eV 





(E=2.3 meV 





Brillouin zone of tellurium and isoenergetic surfaces of holes.





2(1=100 meV 





2(2=126 meV





Conduction band 





Valence band 





(2=63 meV 





kz 





 





SC-(g





Hole concentration p ~ Ni and Nel.active.D for the SC-(g sample. 


X - mobility for the Czhochralski Te crystal.  





� EMBED Origin50.Graph ���





X-ray image of the surface obtained upon cleavage of sample grown by partial remelting of the monocrystal. The arrow shows the starting point of crystallization.











Tellurium crystal solidified in microgravity. 





� EMBED Origin50.Graph ���





Photograph and X-ray images of the tellurium sample grown in space without a seed. 


1-along the length, 


2-along the cross section of the sample. 





Distribution of hole concentration and mobility profiles along the tellurium sample grown without (W) a seed under microgravity conditions and on the Earth.





1





2





Amorphous SiO2 spheres with diameter of 200 ( 250 nm.





Octahedral cavity 





Tetrahedral cavity 





Octahedral cavity





Tetrahedral cavity





Opal structure 











Tellurium cluster lattice in opal with a replica of the octa- and tetrahedral voids as viewed with an electron microscope. Opal crystal filled by Te from a melt under high gas pressure P~3 kBar. Regularly distributed black spots correspond a cluster lattice in the opal matrix (white spots - silica spheres, d~250 nm). 





500 nm





Electron microscope image of tellurium cluster lattice in opal 





� EMBED Word.Document.8 ���





Te





c





10 nm 





Electron microscopy image of an opal silica sphere 





Temperature dependencies of electrical resistivity ( for W-(g (1), W-1g0 (2) and Opal<Te> (3) samples. 1*, 2* the data of measurements in the helium temperature range using platinum contacts fused into a sample. 3* - the repeated measurements. 


1) (((g)>((1g0) and ((Opal<Te>) in the low temperature range. 


•2) High temperature parts of the curves correspond to the transition to the intrinsic conductivity (Energy gap in Te Eg(0)=0.334 eV). 3) The resistivity at helium temperatures is determined by the electrically active and neutral impurities and grain boundaries.





Temperature dependencies of electrical resistivity for Te and Opal<Te> samples. 





� EMBED Origin50.Graph ���





The temperature dependencies of the mobility are attributed to three factors: 


scattering on phonons predominated at temperatures higher than 30K(1/uL ~ T-3/2). 


scattering on charge centers prevailed at low temperatures (1/ui ~ T-3/2/Ni). 


scattering on the defects which limits the maximum value of the hole mobility (1/uD~ND, supposedly independent of temperature).





� EMBED Equation.3 ���





The values of parameters in Eq. 1 for  various Te samples.





(1)





The resulting inverse mobility for the SC-(g sample can be represented by the Matthiessen's rule: 





� EMBED Word.Document.8 ���





** - determined from Tinv of RH.





Temperature dependencies of the Hall coefficient for the monocrystalline SC-(g sample and W-(g microstructure sample, remelted at microgravity conditions, compared with the parameters for W-1g0 opal<Te> samples, made at the earth conditions. (R at 300 K has the negative sign). 





� EMBED Origin50.Graph ���





Temperature dependencies of the reversal hole mobility for the monocrystalline SC-(g sample and W-(g microstructure sample, remelted at microgravity conditions, compared with the parameters of the W-1g0 and opal<Te> samples, made at the earth conditions. Points are for the experimental data, curves are for calculation using the Eq.1 with parameters, showed in Table 1. Straight lines - contributions of  scattering mechanisms for the SC-(g sample. Dashed lines – main contributions of the CND term  to the minima of 1/u value. 





� EMBED Origin50.Graph ���





� EMBED Equation.3 ���





Modulation of the mobility at 77 K and defect concentration ND along the W-(g and W-1g samples, calculated using above equations. For comparison the electrical resistivity profile, (300K(q)  along the W-(g sample is shown. 





� EMBED Equation.3 ���





Determination of the defect concentration ND.





� EMBED Word.Document.8 ���





� EMBED Origin50.Graph ���











.





The behavior of the magnetoresistance for the single crystal SC-1g0, microstructure samples W- Te and Opal<Te> samples at low temperatures.





� EMBED Origin50.Graph ���





� EMBED Origin50.Graph ���





� EMBED Word.Document.8 ���











_1164300405.bin

_1164300529.bin

_1164300576.unknown

_1164300580.bin

_1164300610.unknown

_1164300635.unknown

_1164300608.unknown

_1164300578.doc
For Te:


e0  = 

[image: image1.wmf]e


e


11


2


33


3


0


(


)


= 33.82 


m*/m0=

[image: image2.wmf]m


m


^


×


2


3


|


|


 = 0.156. 


_1029739483.unknown



_1029745445.unknown




_1164300574.unknown

_1164300436.doc


A

B

Ni=p



[image: image1.wmf]D


D


e


*


m


u


1


t


=




ND



Sample



[image: image2.wmf]V


s


cm


K


×


×


2


3


2






[image: image3.wmf]2


3


K


cm


s


V


×


×


×




cm-3



[image: image4.wmf]cm


V


s


2


1


×


æ


è


ç


ö


ø


÷


-




cm-3



SC-(g 

3Ч10-7

4.9Ч10-19

4.1Ч1014

9.3Ч10-6

7.7Ч1015



W-(g 

3Ч10-7

4.9Ч10-19

1.2Ч1015

1.0Ч10-3

8.3Ч1017



W-1g0

3Ч10-7

4.9Ч10-19

1.1Ч1015

6.0Ч10-4

5.0Ч1017



Opal<Te>

3Ч10-7

4.9Ч10-19

1.8(1014**

1.5Ч10-1

1.2Ч1020



_1029739478.unknown



_1030721448.unknown



_1155412982.unknown



_1029739476.unknown




_1164300470.bin

_1164300435.unknown

_1164300247.bin

_1164300352.doc








_1155674776.unknown



_1155674936.unknown




_1164300218.bin

